## Slide 1
80℃ oil bath (oil level should be higher than the CMOH growing solution)
FTO (3x1 cm2)
1.5 cm
1.5 cm
250 mL beaker
500 rpm
(Blue Hot plate turn to 3)
1X CMOH Standard Growing Method
Time: 15 min
Precursor: 150 mL H2O + 6 mmol Co(OAc)2 + 2 mmol KMnO4
Procedure: Put the room-temp. beaker into a 80℃ oil bath
Position of substrate: hung on beaker side wall with half immerse.
Blue Hot plate
Brand: RCT basic
Front
Back

## Slide 2
一倍 CMOH 薄膜標準生長步驟
80℃ 油浴 (油高度須高於 CMOH 生長溶液)
FTO (3x1 cm2)
1.5 cm
1.5 cm
250 mL 燒杯
500 rpm
藍色加熱板(轉到3)
時間: 15 分鐘
生長液: 150 mL H2O + 6 mmol Co(OAc)2 + 2 mmol KMnO4
生長步驟: 將室溫燒杯置入 80℃ 油浴
基板放置位置: 掛至於燒杯壁上，一半浸泡一半露於空氣中
藍色加熱板
品牌:RCT basic數位式電磁加熱攪拌器
正面
背面