## Slide 1: Your Topic 1. 含氮GO的水熱合成: 用urea調控pH 2. MB在可見光催化
Your Name
實驗紀錄簿編號
報告時間 (i.e. 5. 31. 2023)
From 5. 24. 2023 to 5. 30. 2023

## Slide 2: Last Week
What are the tasks to do?

## Slide 3: Goal of this week
What’s the goal or motivation to do in this week?

## Slide 4: 合成 (Preparation)
Sample (Name) | Code (Lab notebook) | Method | Description | Characterization | Others

## Slide 5: Preparation (合成)
Sample (Name) | Code (Lab notebook) | Method | Description | Characterization | Others
Cobalt manganese oxide (CMO) | CCM-35 | hydrothermal | Low cobalt content (vs. CCM-36) | XRD, SEM, EDS | P. 35
CMO-100 | CCM-36 | hydrothermal | High cobalt content (vs. CCM-35) 再現性測試 | XRD | P. 36 in your lab note
Nitrogen-doped G.O. | KGG-89 | Hummers | 我使用新的石墨粉 (vs KGG-87) | Not yet | 好像失敗了，重作一次再比較 (KGG-90)
單層石墨烯 | LGM-56 | CVD | 新的銅片，時間由原來 20min 縮短到 5min (vs LGM-20) | Raman, 光學顯微鏡相片 (好像是多層) | 時間縮短破洞好像變多
重點說明
鑑定結果
此實驗哪裡不同?
為何作這個實驗
鑑定結果列在後續投影片

## Slide 6: Procedure / Methodology

## Slide 7: Results of Samples
Your Results Here
Description
What are we seeing?
Description
Comparison?
Description
Where are these results?
Description
Where are these results?

## Slide 8: Results (SEM) of Samples (CMO-100)
Description
After GO hybridization
Description
Before GO hybridization
Description
Path: chc/結果/SEM/gcmo-20-2
Description
Path: chc/結果/SEM/cmo-100C-12
Exp. Code
CCM-36
Exp. Code
CCM-10
File Path of figures or data

## Slide 9: 單層石墨烯 (新銅片) of YCG-3
光學顯微鏡圖 (OM of something; if more than one)
新銅片作的石墨烯
表面不乾淨有大量破洞
Patch: YCG/結果/Raman/OM-5
光學顯微鏡圖 (OM)
新銅片作的石墨烯
表面不乾淨有大量破洞
YCG-3
Path: YCG/結果/Raman/spec/YCG-3-5
File Path of figures or data

## Slide 10: What I Learn
This page is for undergraduate students.

## Slide 11: Conclusion
What is the meaning of your data?
What is the critical message for your next move?
What do we learn from your data?

## Slide 12: Next
What are you going to do next?

## Slide 13: Paper
No | Title | Journal | Year | Remark
1 | Activation Energy Assessing Potential-Dependent Activities and Site Reconstruction for Oxygen Evolution | ACS Energy Letters | 2022 | Done
2 |  |  |  | 
3 |  |  |  |